## Slide 1: Data-analysis of Al-reference samples
From SilverLIBS
(prototype with Litron-laser and IBSEN spectrometer)

## Slide 2: Samples
Elements of interest:
  Si, Fe, Mg, Zn, Cu, Mn
Ref. element:
  Al

## Slide 3: Samples

## Slide 4: Steps
Identify peaks
  Since we used gated spectrometer ionic lines are not expected
Sort spectra to use
  Sort on Al-peak: 308,24
  Offset (zero-level): 100
  Remove baseline and
  Calibration curves:
    Minimum intensity 1000 (and saturation 60000)
    Minumim intensity 5000 (and saturation 60000)

## Slide 5: Chosen peaks (chosen=1, possible other=0)
Si | Mg II | Zn | Zn | Mn | Mn | Mn | Mn | Fe | Fe | Fe | Fe | Fe | Fe | Fe | Cu | Cu | Al | Al | Al, | Al,
1 | 1 | 0 | 1 | 1 | 0 | 0 | 0 | 0 | 1 | 0 | 0 | 0 | 0 | 0 | 1 | 0 | 1 | 0 | 0 | 0
--------- | --------- | ---- | ---- | --------- | --------- | --------- | ---- | --------- | --------- | --------- | ---- | --------- | --------- |  | --------- | --------- | --------- | --------- | --------- | ---------
288,18 | 383,82 | 330,24 | 334,50 | 403,10 | 403,30 | 403,40 | 404,10 | 257,57 | 357,00 | 372,00 | 373,43 | 373,69 | 404,58 | 427,10 | 324,73 | 327,37 | 308,24 | 309,31 | 394,41 | 396,15

## Slide 6: Example, identification of peaks

## Slide 7: Example, sorting: 038 - Gränges al 6958-v-336

## Slide 8: Si 288,18 / Al 308,24
Reference intensity: >1000 cts
Reference intensity: >5000 cts

## Slide 9: Mg 383,82 / Al 308,24
Reference intensity: >1000 cts
Reference intensity: >5000 cts

## Slide 10: Zn 334,50 / Al 308,24
Reference intensity: >1000 cts
Reference intensity: >5000 cts

## Slide 11: Mn 403,10 / Al 308,24
Reference intensity: >1000 cts
Reference intensity: >5000 cts

## Slide 12: Fe 357,0 / Al 308,24
Reference intensity: >1000 cts
Reference intensity: >5000 cts

## Slide 13: Cu 324,73 / Al 308,24
Reference intensity: >1000 cts
Reference intensity: >5000 cts